# Supplementary Information

# Controlled-synthesis of Hierarchical NiCo2O4 anchored on carbon nanofibers mat for Free-Standing and Highly-Performance supercapacitors

*M Hussein El-Shafei1,2, Ahmed G. El-Deen3, Ahmed Abd El-Moneim2,4, Amr Hessein2,5

1Production engineering and mechanical design department, Mansoura University, El-Mansoura 35516, Egypt.

2Graphene Center of Excellence for Energy and electronic Applications, Egypt-Japan University of Science and Technology, Alexandria 21934, Egypt.

3Renewable Energy Science and Engineering Department, Faculty of Postgraduate Studies for Advanced Sciences (PSAS), Beni- Suef University, Beni-Suef  62511, Egypt

4Institute of Basic and Applied Sciences, Egypt-Japan University of Science and Technology, New Borg El Arab, Alexandria 21934, Egypt.

5Department of Mathematical and Physical Engineering, Faculty of Engineering (Shoubra), Benha University, Cairo 11614, Egypt.

*Corresponding author:

*(M. Hussein El-Shafei), Full name: Mohamed Hussein Issa El-Shafei, Mob: +201009919969,      E-mail: m_hussein@mans.edu.eg

Fig. S1: The equivalent circuit used to fit the electrochemical impedance spectroscopy (EIS) data. RESR is the series equivalent resistance, RCT is the charge transfer resistance, C is the capacitance element, and W is the Warburg element accounting for the resistance to the electrolyte diffusion.

Fig. S2: XRD patterns for CNFs, NiO samples and the NiO:CNFs hybrid nanocomposite. The pattern of the NiO:CNFs nanocomposite showed peaks of NiO has pure cubic phase  (JCPDS, No. 47-1049) are superimposed on the CNFs pattern.

Fig. S3: SEM micrographs for (a, a1) NiO 1:2 CNFs, (b,b1) NiO 1:1 CNFs, (c,c1) NiO 2:1 CNFs nanocomposites obtained at two magnifications.

Fig. S4: XRD patterns for CNFs, Co3O4 samples and the Co3O4:CNFs hybrid nanocomposite. The pattern of the NiO:CNFs nanocomposite showed peaks of Co3O4  has pure cubic phase  (JCPDS No. 42-1467) are superimposed on the CNFs pattern.

Fig. S5: SEM micrographs for (a, a1) Co3O4 1:2 CNFs, (b,b1) Co3O4 1:1 CNFs, (c,c1) Co3O4 2:1 CNFs nanocomposites obtained at two magnifications.

Fig. S6: Specific capacitances calculated from GCD measurements at 1 A g-1 for all symmetric supercapacitors fabricated from all synthesised NiO:CNFs, Co3O4:CNFs, and NiCo2O4:CNFs hybrid nanocomposites at different loading ratios.